The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep21tp-2nv.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Toughened Epoxy Polysulfide Hybrid Offers Advanced Chemical Resistance

Master Bond EP21TP-2NV is a two part epoxy polysulfide formulated for use as an adhesive, sealant and potting system. It withstands prolonged exposure to many harsh chemicals including fuels, oils, hydrocarbons and hydraulic fluids. It is also fully RoHS compliant, meeting RoHS3 Directive (EU) 2015/863.

EP21TP-2NV offers an elongation between 40-80% at room temperature and superior toughness with a tensile strength of 3,000-4,000 psi. It resists aggressive thermal cycling over the service temperature range of -80°F to +250°F [-62°C to +121°C]. With a dielectric constant of 3.7 at 60 Hz, the system provides excellent electrical insulation properties.

Master Bond EP21TP-2NV cures at room temperature in 48-72 hours to form a rigid material with a Shore D hardness measuring 60-65. A unique feature of EP21TP-2NV is its ability to cure softer with the addition of heat. For example, when cured at 200°F for 2-3 hours its hardness decreases to 15-20 Shore D.

EP21TP-2NV bonds well to a variety of substrates such as metals, glass, ceramics and many rubber and plastic materials. This compound is available in standard size containers from ½ pint, pint, quart and gallon kits as well as specialty packaging including double barrel syringes and gun dispensers.

Master Bond Chemically Resistant Adhesive Systems

Master Bond EP21TP-2NV is a two part epoxy polysulfide featuring superior chemical and thermal cycling resistance while maintaining tough, flexible bonds. Read more about Master Bond’s chemically resistant adhesive systems at https://www.masterbond.com/properties/chemical-resistance or contact Tech Support. Phone: +1-201-343-8983  Fax: +1-201-343-2132  Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep21tp-2nv

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #