The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep40med

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Epoxy with High Elongation Passes ISO 10993-5 Certification for Cytotoxicity

Master Bond EP40Med, a two part epoxy system, combines toughness and a low tensile modulus while still providing a relatively high lap shear strength. It meets the requirements of ISO 10993-5 testing and is therefore considered to be non-cytotoxic. This compound can be used for bonding, sealing, coating and encapsulating.

EP40Med resists sterilization to gamma, EtO, chemicals, and liquid disinfectants. It is recommended for use in medical device manufacturing and repair for both disposable and reusable instruments. EP40Med is an effective adhesive for applications where toughness and flexibility along with good structural strength are needed. The formulation bonds well to polycarbonates, acrylics, metals, ceramics and composites. This flexible epoxy has an elongation of 80-90%, a lap shear strength of 1,600 to 1,800 psi and a low tensile modulus of 25,000 to 50,000 psi. EP40Med is a reliable electrical insulator with a volume resistivity over 1012 ohm-cm.

This system is easy to use with a one to one mix ratio by weight or volume and a low to moderate viscosity of both parts A and B. The working life of a mixed 100 gram batch is approximately 120-150 minutes. The optimal cure schedule is overnight at room temperature followed by a post cure for 2- 3 hours at 150°F. The product is available in 1/2 pint, pint, quart, and gallon kits. Specialty packaging is available in gun dispensers and premixed and frozen syringes.

Master Bond Biocompatible Adhesives

Master Bond EP40Med is a two component, biocompatible epoxy system formulated for medical device manufacturing applications. Read more about Master Bond’s biocompatible adhesives that pass USP Class VI and ISO 10993-5 certifications at https://www.masterbond.com/properties/biocompatible-adhesives or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/newsrelease/ep40med

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #