-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep51cc .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Fast Setting, Two Component Epoxy Color Coded for Proper Mixing

Master Bond EP51CC is a two component, fast setting epoxy with a color coding system where Part A is white and Part B is black. The two parts combine into a uniform gray color paste, which indicates proper mixing. This fast curing, non-drip compound is ideal for bonding and sealing applications with a forgiving mix ratio of one to one by weight or volume.

This high performance epoxy has a rapid set up time, convenient handling, and good physical properties. It sets up very quickly at room temperature, with a working life of 3-5 minutes for a mixed 50 gram batch. The exact fixture time in an application context can vary from a few minutes to several hours, depending on multiple factors including, but not limited to the size of the components, the substrates being bonded, curing temperature and the amount of adhesive applied. An interesting feature of EP51CC is the role that the cure schedule plays in the bond strength. For example, it offers a lap shear strength of 700-800 psi when cured at room temperature for 24 hours, but when cured at room temperature for 8 hours followed by 3 hours at +250°F, its lap shear strength increases to 2,300-2,500 psi. It features high strength bonds to a variety of substrates including metals, composites, glass, ceramics, vulcanized rubbers, and many plastics with a tensile modulus of 100,000-150,000 psi at room temperature. EP51CC is electrically insulative with a volume resistivity of >1014 ohm-cm and a dielectric strength of 450 volts/mil.

Formulated for temperatures ranging from 4K to +250°F, this epoxy is also suitable for challenging cryogenic applications. EP51CC is available in ounce kits, half pint kits, pint kits, quart kits, gun applicators, and FlexiPaks® for ease of use.

Master Bond Fast Curing Adhesives

EP51CC is a fast curing, two component epoxy featuring a color coded system where Part A is white and Part B is black to ensure proper mixing. This non-drip compound is ideal for bonding and sealing applications with a forgiving mix ratio of one to one by weight or volume. Read more about Master Bond’s fast curing adhesives at https://www.masterbond.com/properties/fast-curing-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep51cc

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #