-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at: https://www.masterbond.com/newsrelease/supreme-42ht-2nd-black.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Electrically Insulative, Toughened Epoxy Meets NASA Low Outgassing Specifications

Master Bond Supreme 42HT-2ND Black is a two-part, non-drip epoxy system designed for bonding, sealing and coating applications. It is capable of withstanding temperatures up to 450°F (232°C), and provides a glass transition temperature (Tg) of 130-135°C. The material meets NASA low outgassing standards and is recommended for applications that require vacuum compatibility.

Supreme 42HT-2ND Black is electrically insulative with a volume resistivity greater than 1014 ohm-cm. This compound has a Shore D Hardness of 75-85 at 75°F and withstands rigorous thermal cycling. It passed damp heat reliability testing for 1,000 hours at 85°C and 85% relative humidity. It offers a high strength profile, with a tensile strength of 9,000-10,000 psi and a tensile modulus of 300,000-350,000 psi at 75°F.

With a forgiving mix ratio of 100 to 40 by weight or 100 to 50 by volume, this paste consistency material can be easily applied with the use of a gun dispenser or spatula. It cures at ambient temperature in 2-3 days, or faster with the addition of heat. Adding heat not only speeds up the curing process but also optimizes the overall performance properties. Supreme 42HT-2ND Black is available in standard packaging, double barrel cartridges for gun kits, as well as pre-mixed and frozen syringes.

Master Bond Electrically Insulating, Low Outgassing Adhesives

Master Bond Supreme 42HT-2ND Black is a NASA low outgassing, electrically insulating, two-part epoxy system used for bonding, sealing and encapsulating. It passes 85°C/85% RH testing, which helps to determine the expected operating life for devices in many critical aerospace, optical, electronic and optoelectronic applications.  Read more about Master Bond’s electrically insulating adhesives at https://www.masterbond.com/properties/electrically-insulative-adhesive-systems  or contact Tech Support.

Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/supreme-42ht-2nd-black.

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #