This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep21arht.

----------------------------------

FOR IMMEDIATE RELEASE

Long-Lasting Epoxy System Resists Fuels,

Acids & Other Aggressive Chemicals

HACKENSACK, NJ – October 21, 2010 – Developed for coating and lining storage tanks, piping, scrubbers, and processing equipment in the chemical industry, Master Bond EP21ARHT features outstanding chemical, fuel, and acid resistance. Also widely used in electronic, electrical, and metalworking industries, it can even successfully withstand immersion to 96-98% sulfuric acid and 20% hydrochloric acid for more than a year.

This two component epoxy cures at room temperature with minimal shrinkage, or more rapidly at elevated temperatures. Once fully cured, it produces a bond strength greater than 2,200 psi. EP21ARHT can be thermally cycled over the wide temperature range of -60ºF to +400ºF. This system features superior electrical insulation capabilities with a dielectric strength of 440 volts/mil and a low coefficient of thermal expansion of 40-45x10-6 in/in/ºC. EP21ARHT bonds well to metals, ceramics, glass and many plastics.

This epoxy offers a convenient non-critical 2 to 1 mix ratio by weight. It is color coded, with part A being clear and part B amber. Master Bond Polymer System EP21ARHT is available for purchase in pint, quart, gallon, and 5 gallon container kits.

Master Bond Chemically Resistant Epoxies

Master Bond’s chemically resistant EP21ARHT is especially designed for coating, bonding, lining, and sealing in applications where exceptional acid resistance is required. Read more about Master Bond’s chemically resistant epoxy systems at http://www.masterbond.com/lp/tabs/tp_pp_chemresist.html or contact Technical Support by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at technical@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #